# GLOW TIP SHEET

## GLOW PIGMENT

- MUST BE FULLY ENCASED INSIDE GLASS.  CUT YOUR CLEAR CAP LARGE ENOUGH TO FULLY ENCAPSULATE ALL EDGES AND TRAP PIGMENT INSIDE.

- PIGMENT CAN HANDLE TEMPERATURES UP TO 1800F

- KEEP PIGMENT DRY, EVEN DURING/AFTER COLDWORKING

- CAN BE MIXED WITH GLASS POWDER FOR CASTING ETC., BUT DO NOT EXCEED 30% PIGMENT TO GLASS RATIO

- CAN BE MIXED WITH ANY BINDER, GLAZE, OVERGLAZE OR ANY OTHER CLEAR MEDIUM USED FOR HOTWORKING.

- HANDLE PIGMENT AS IF IT WERE GLASS POWDER (USE PROPER BREATHING FILTER AND VENTILATION)

- STORE PIGMENT IN A COOL DRY PLACE

### GLOW DECALS

- MADE TO BE FIRED ONTO THE SURFACE OF GLASS FIRST, BUT THEN CAN BE CLEAR-CAPPED DURING SECOND FIRING

- SOAK DECAL IN WATER UNTIL IT EASILY SLIDES OFF PAPER AND ONTO GLASS

- ALL AREAS MUST BE FLATTENED ONTO THE GLASS AS IT WILL NOT SETTLE LATER.

- REMOVE ALL MOISTURE PRIOR TO FIRING (OVERNIGHT DRYING IS RECOMMENDED)

- DECALS CAN HANDLE TEMPERATURES TO 1400F ONLY

- ONCE BAKED ON, DECAL CAN GET WET (BAKE TO AT LEAST 1250 FOR 10 MINUTES)

- DECALS CAN BE FIRED ONTO GLAZED CERAMICS (FIRE TO 1250 FOR 10 MINUTUES MINIMUM)

- DECALS CAN BE FIRED ONTO TUBING AND/OR OTHER 3 DIMENSIONAL OBJECTS (FIRE TO 1250 FOR 10 MINUTES MINIMUM)